## SUBSTITUTE MATERIAL (JIS, BS, DIN ) FOR ASTM SPECIFICATION

Abter steel pipe company , https://www.abtersteel.com

CONTENTS

Section												Page

1.	Scope

2.	Basis

3.	Additional Requirements

4.	Table

5.	Table 1,	Plates

6.	Table 2,	Pipes

7.	Table 3,	Tubes

8.	Table 4,	Forging

9.	Table 5,	Castings

10.	Table 6,	Bolts and Nuts

11.	Table 7,	Bars and Shapes

12	Table 8,	Piping Fittings

13.	Table 9,	Nonferrous Materials

- SCOPE

This specification lists the Japanese Standard (JIS, JPI),British Standard (BS), and Deutshe Industrie Normen (DIN) substitutes for ASTM Specifications relating to materials for plates,	pipes, tubes, forging, castings, bolts and nuts, bars and shapes, piping fittings, and nonferrous materials, in general use.

- BASIS

These substitutes are not necessarily identical to the ASTM Specifications, but are equal in terms of alloy content and have a nearly equal or higher ultimate tensile strength; exceptions to this are underlined.

- ADDITIONAL REQUIREMENTS

The requirements of the ASTM Specifications not covered by the substitute specifications are noted in the Tables, with footnotes given on Section 4.

- TABLE

Substitute materials are shown in the following Tables 1 to 9.

STANDARD SPECIFICATION

Table 1 PLATE

| ASTM | JIS | BS | DIN |
| --- | --- | --- | --- |
| A-36 |  |  |  |
| Structural Steel |  |  |  |
|  | G 3101 SS400 | 4360 Gr 40A (1) | 17100 St44-2 |
|  | G 3105 SM400A | 4360 Gr 438 (1) | 17100 St44-3 |
| A-131 |  |  |  |
| Structural Steel for Ships |  |  |  |
| Gr A | G 3106 SM400A | 4360-40B | 17100 St44-3 |
| Gr B | G 3106 SM400B | 4360-40B | --- |
| Gr CS | G 3105 SM400CN | 4360-40E | --- |
| Gr D | G 3105 SM400C (2) | 4360-40E | --- |
| Gr E | G 3105 SM40OCN | 4360-40E | --- |
| A-167 |  |  |  |
| Stainless arid Heat-Resisting |  |  |  |
| Chromium,-Nickel Steel Plate, |  |  |  |
| Sheet, and Strip |  |  |  |
| Type 302 | G 4304 SUS302 (3) | --- | 17440/1 X10CrNiS189 |
| Type 304 | G 4304 SUS304 (3) | 1449-304S31 | 17440/1 X5CrNi1810 |
|  |  | 1501-304S15 |  |
| Type 304L | G 4304 SUS304L (3) | 1501-304S12 | 17440/1 X2CrNi1911 |
|  |  | 1449-304S11 |  |
| Type 310S | G 4304 SUS310S (3) | 1501-310S24 | --- |
|  |  | 1449-310S24 | --- |
| Type 316 | G 4304 SUS316 (3) | 1501-316S16 | 17440/1 X5CrNiMo17122 |
|  |  | 1449-316S31 |  |
| Type 316L | G 4304 SUS316L (3) | 1501-316S12 | 17440/1 X2CrNiMo17132 |
|  |  | 1449-316S11 |  |
| Type 321 | G 4304 SUS321 (3) | 1501-321S12 | 17440/1 X6CrNiTi1810 |
|  |  | 1449-321S31 |  |
| Type 347 | G 4304 SUS347 (3) | 1501-347S17 | 17440/1 X6CrNiNb1810 |
|  |  | 1449-347S31 |  |

Note (1): Specify mechanical properties, test and inspection in accordance with ASTM.

Note (2): Plates over 1-3/8 Inches (35 m-n) in thickness shall be normalized.

Note (3): For cold rolled sheet and strip, use corresponding SUS-CP and SUS-CS steels, according to JIS G 4305 and G 4307, respectively.

| STANDARD SPECIFICATION ASTM | JIS | BS | DIN |
| --- | --- | --- | --- |
| A-176 |  |  |  |
| Stainless and Heat Resisting |  |  |  |
| Chromium Steel Plate, Sheet, |  |  |  |
| And Strip |  |  |  |
| Type 403 | G 4304 SUS403 (1) | 14-09-403 S17 S2) | --- |
|  |  | 1501-403 S17 l2) | --- |
| Type 405 | G 4304 SUS405 (1) | 1449-405 S17 | 17440/1 X6CrAl13 |
|  |  | 1501-405 S17 | --- |
| Type 410 | G 4304 SUS410 (1) | 1449-410 S21 | 17440/1 X10Cr13 |
| Type 4105 | G 4304 SUS410S (1) | --- | 17440/1 X6Cr13 |
| A-203 |  |  |  |
| Pressure Vessel Plates, |  |  |  |
| Alloy Steel, Nickel |  |  |  |
| Gr A | G 3127 SL2N255 | --- | --- |
| Gr D | G 3127 SL3N255 | 1501-503 | --- |
| Gr E | G 3127 SL3N275 | --- | 17280 10Ni14 |
| Gr F | G 3127 SL3N440 | --- | --- |
| A-204 |  |  |  |
| Pressure Vessel Plates, |  |  |  |
| Alloy Steel, Molybdenum |  |  |  |
| Gr A | G 3103 S64SOM | --- | SEL 16 Mo5 |
|  |  |  | 17155 15 Mo3 |
| Gr B | G 3103 SB48M | --- | SEL 16 Mo5 |
| Gr C | --- | --- | --- |
| A-240 |  |  |  |
| Heat-Resisting Chromium and |  |  |  |
| Chromium-Nickel Stainless |  |  |  |
| Steel Plate, Sheet, and Strip |  |  |  |
| for Pressure Vessels |  |  |  |
| Type 304 | G 4304 SUS304 (1) | 1501-304S15 | 17440/1 X5CrNi1810 |
| Type 304H | --- | 1501-304S49 | --- |
| Type 304L | G 4304 SUS304L (1) | 1501-304S12 | 17440/1 X2CrNi1911 |
| Type 316 | G 4304 SUS316 (1) | 1501-316S16 | 17440/1 X5CrNiMo17122 |
| Type 316H | --- | 1501-316S49 | --- |
| Type 316L | G 4304 SUS316L (1) | 1501-316S12 | 17440/1 X2CrNiMo17132 |
| Type 317 | G 4304 SUS317 (1) |  |  |
| Type 317L | G 4304 SUS317L (1) | --- | 17440/1 X2CrHiMo18164 |

Note (1):	For cold rolled sheet and strip, use corresponding SUS-CP and SUS-CS steels, according to JIS G 4305 and G4307, respectively.

Note (2):	Recognize lower minimum tensile or yield strengths of the underlined substitute materials in design consideration, or specify minimum tensile and yield strengths per ASTM.

STANDARD SPECIFICATION

| ASTM | JIS | BS | DIN |
| --- | --- | --- | --- |
| Type 321 | G 4304 SUS321 (1) | 1501-321S12 | 17440/1 X6CrNiTi1810 |
| Type 321H | --- | 1501-321S49 | --- |
| Type 347 | G 4304 SUS347 (1) | 1501-3-07S17 | 17440/1 X6CrNiNb1810 |
| Type 347H | --- | 1501-347S49 | --- |
| Type 405 | G 4304 SUS405 (1) | 1501-405S17 | 17440/1 X6CrAl13 |
| Type 410 | G 4304 SUS410 (1) | --- | 17440/1 X10Cr13 |
| Type 410S | G 4304 SUS410S (1) | --- | 17440/1 X6Cr13 |
| Type 430 | G 4304 SUS430 (1) | --- | 17440/1 X6Cr17 |
| A-263 |  |  |  |
| Corrosion-Resisting |  |  |  |
| Chromium Steel-Clad |  |  |  |
| Plate, Sheet, and |  |  |  |
| Strip |  |  |  |
|  | G 3601 (2) | --- | 17440/1 |
| A-264 |  |  |  |
| Stainless Chromic-Nickel Steel- |  |  |  |
| Clad Plate, Sheet, and Strip |  |  |  |
|  | G 3601 (2) | 3740 (2) | 17440/1 |
| A-265 |  |  |  |
| Nickel and Nickel-Base |  |  |  |
| Alloy-Clad Steel Plate |  |  |  |
|  | G 3602 (2) | --- | 17743 NiCu30Fe |
| A-283 |  |  |  |
| Low and Intermediate Tensile |  |  |  |
| Strength Carbon Steel Plates, |  |  |  |
| Shapes, and Bars |  |  |  |
| Gr A | G 3101 SS330 | 4360 Gr 40A/B/C | 17100 St33 |
| Gr B | G 3101 55330 | 4360 Gr 40A/B/C | 17100 St33 |
| Gr C | G 3101 SS400 | 4360 Gr 40D | 17100 St44-2 |
| Gr D | G 3101 SS400 | 4360 Gr 43A/B/C/D | 17100 St44-2 |

Note (1):	For cold rolled sheet and strip, use corresponding SUS-CP and SUS-CS steels, according to JIS G 4305 and G4307, respectively.

Note (2): Specify mechanical properties, test and inspection in accordance with ASTM.

STANDARD SPECIFICATION

| ASTM | JIS | BS | DIN |
| --- | --- | --- | --- |
| A-285 |  |  |  |
| Pressure Vessel Plates, |  |  |  |
| Carbon Steel, Low-and |  |  |  |
| Intermediate-Tensile |  |  |  |
| Strength |  |  |  |
| Gr A & B | --- | 1501-151 Gr 360 | 17155 H I |
| Gr C | G 3103 S8410 | 1501-151 Gr 430 | 17155 H II |
| A-299 |  |  |  |
| Pressure Vessel Plates, Carbon |  |  |  |
| Steel, Manganese Silicon |  |  |  |
|  | G 3115 SPV355 | --- | 17102 StE355 |
| A-302 |  |  |  |
| Pressure Vessel Plates, Alloy Steel |  |  |  |
| Manganese-Molybderalm and |  |  |  |
| Manganese-Holybdenum- |  |  |  |
| Nickel |  |  |  |
| Gr A | G 3119 SBV1A | --- | --- |
| Gr B | G 3119 SBV1B | --- | --- |
| Gr C | G 3119 SBV2 | --- | --- |
| Gr D | G 3119 SBV3 | --- | --- |
| A-387 |  |  |  |
| Pressure Vessel Plates, Alloy Steel |  |  |  |
| Chromium-Molybdenum |  |  |  |
| Gr 2 Class 1 | G 4109 SCMV1 | --- | --- |
| Gr 11 Class 1 | G 4109 SCMV3 | 1501-621 | --- |
| Class 2 | G 4109 SCMV3 | 1501-621 |  |
| Gr 12 Class 1 | G 4109 SCMV2 | 1501-620 | 17155 13CrMo44 |
| Class 2 | G 4109 SCMV2 | 1501-620 | --- |
| Gr 21 Class 1 | G 4109 SCMV5 | --- | --- |
| Gr 22 Class 1 | G 4109 SCMV4 | 1501-622 Gr 515 | 17155 10CrMo910 |
| Class 2 | G 4109 SCMV4 | 1501-622 Gr 515 | --- |
| Gr 5 Class 1 | G 4109 SCMV6 | --- | SEW590 12CrMo195 |
| Class 2 | G 4109 SCMV6 | --- | --- |
| Gr 9 Class 1 | --- | --- | --- |
| Class 2 | --- | --- | --- |

| ASTM | JIS | BS | DIN |
| --- | --- | --- | --- |
| A-442 |  |  |  |
| Pressure Vessel Plates, Carbon |  |  |  |
| Steel, Improved Transition |  |  |  |
| Properties |  |  |  |
| Gr 55 | --- | 1501-151 Gr 400 | SEW 680 TTSt41N |
|  |  | 1501-161 Gr 400 |  |
|  |  | 1501-224 Gr 400 |  |
| Gr 60 | G 3115 SPV235 | 1501-151 Gr 430 | --- |
|  |  | 1501-161 Gr 430 |  |
|  |  | 1501-224 Gr 430 |  |
| A-516 |  |  | - |
| Pressure Vessel Plates, Carbon |  |  |  |
| Steel, for Moderate and Lower |  |  |  |
| Temperature Service |  |  |  |
| Gr 55 --- |  | 1501-161 Gr 400 | 17155 H I |
|  |  | 1501-224 Gr 400 |  |
| Gr 60 | G 3118 SGV410 | 1501-161 Gr 430 | 17155 H II |
|  |  | 1501-224 Gr 430 |  |
| Gr 65 | G 3118 SGV450 | 1501-224 Gr 460 | 17155 17Mn4 |
| Gr 70 | G 3118 SGV480 | 1501-224 Gr 490 | 17155 19Mn6 |

Note (1):	Recognize lacer minimum tensile or yield strengths of the underlined substitute materials in design consideration,

or specify minimum tensile and yield strengths per ASTM.

STANDARD SPECIFICATION

| Note (1): Recognize loner minimum tensile or yield strengths of the underlined substitute materials in design consideration, or specify minimum tensile and yield strengths per ASTM. ASTM | JIS | BS | DIN |
| --- | --- | --- | --- |
| A-533 I |  |  |  |
| Pressure Vessel Plates,Alloy Steel |  |  |  |
| Quenched and Tempered |  |  |  |
| Manganese- Molybdenum and |  |  |  |
| Manganese- Molybdenum Nickel |  |  |  |
| Type A Class 1 | G 3120 SQV1A | --- | --- |
| Class 2 | G 3120 SQV1B | --- | --- |
| Type B Class 1 | G 3120 SQV2A | --- | --- |
| Class 2 | G 3120 SQV2B | --- | --- |
| Type C Class 1 | G 3120 SQV3A | --- | --- |
| Class 2 | G 3120 SQV3B | --- | --- |
| A-537 |  |  |  |
| Pressure Vessel Plates, Heat- |  |  |  |
| Treated, Carbon-Manganese- |  |  |  |
| Silicon Steel |  |  |  |
| Class 1 | G 3115 SPV355N | 1501-224 Gr 490 (1) | 17155 19Mn6 |
|  |  |  | 17102 StE355 |
| Class 2 | G 3115 SPV450Q | --- | --- |
| A-570 |  |  |  |
| Steel, Sheet and Strip, Carbon, |  |  |  |
| Hot-Rolled, Structural Quality. |  |  |  |
| Gr 30 | G 3101 SS330 | 1449-HR 34/20 (1) | 17100 St33 |
| Gr 33 | G 3101 SS400 | 1449-HR 37/23 | 17100 St44-2 |
| Gr 36 | G 3101 SS400 | 1449-KR 37/23 | 17100 St44-2 |
| Gr 40 | G 3101 SS400(1) | 1449-HR 43/25 | 17100 St44-2 |
| Gr 45 | G 3101 SS490 | 1449-HR 43/25 (1) | 17100 St52-3 |
| Gr 50 | G 3101 SS490(1) | 1449-HR 50/35 | 17100 St52-3 |
| A-611 |  |  |  |
| Steel, Sheet, Carbon, Cold-Rolled |  |  |  |
| Structural Quality |  |  |  |
| Gr B | G 3141 SPCC (2) | --- | --- |
| Gr C | G 3141 SPCC (2) | --- | 1623.1 St12 |
| Gr D | G 3141 SPCC (2) | --- | --- |

Note (2): 	Specify mechanical properties, test and inspection in accordance with ASTM.

STANDARD SPECIFICATION

| Note (1): Specify Impact Test requirement per ASTM. ASTM | JIS | BS | DIN |
| --- | --- | --- | --- |
| A-652 |  |  |  |
| Pressure Vessel Plates, Carbon |  |  |  |
| Manganese, for Moderate and |  |  |  |
| Lower Temperature Service |  |  |  |
| Gr A | G 3126 SLA235 (1) | --- | --- |
| Gr B | G 3126 SLA325 (1)(2) | --- | 17102 EStE315 |
| Gr C | G 3126 SLA360 (1) | --- | 17102 EStE355 |

Note (2):	Recognize lager minimum tensile or yield strengths of the underlined substitute materials in design consideration, or specify minimum tensile and yield strengths per ASTM.

STANDARD SPECIFICATION

Table 2 PIPE

| Note (1): Specify carbon, manganese, or silicon contents to accordance with ASTM. ASTM | JIS | BS | DIN |
| --- | --- | --- | --- |
| A-53 |  |  |  |
| Pipe, Steel, Black and Hot-Dipped |  |  |  |
| Zinc-Coated Welded and Seamless |  |  |  |
| Type F | G 3452 SGP | 1387 | 1615 St33 |
| Gr A | G 3454 STPG370 | 3601 ERW360 | 1626 St37.0 |
|  |  | S360 | 1629 St37.0 |
| Gr B | G 3454 STPG410 | 3601 ERW410 | 1626 St44.0 |
|  |  | S410 | 1629 St44.0 |
| A-105 |  |  |  |
| Seamless Carbon Steel Pipe for |  |  |  |
| High-Temperature Service |  |  |  |
| Gr A | G 3456 STPT370 | 3602 HFS360 | 17175 St35.8 |
|  |  | 3602 CFS360 |  |
| Gr 8 | G 3.455 STPT410 | 3602 HFS410 | 17175 St45.8 |
|  |  | 3602 CFS410 |  |
| Gr C | G 3456 STPT480 | 3602 HFS460 | 17175 St45.8 |
|  |  | 3602 CFS460 |  |
| A-134 |  |  |  |
| Pipe, Steel, Electric-Fusion (Arc)- |  |  |  |
| Welded (Size NPS 16 and over) |  |  |  |
| Material |  |  |  |
| A 283 Gr A – D | G 3457 STPY400 | 3602 SAW410 | --- |
|  |  | 3601 SAW410 |  |
| A 285 Gr A – C | G 3457 STPY400(1) | --- | -- |
| A 570 Gr 30 – 40 | G 3457 STPY400 (1)(2) | --- | -- |
| A 36 | G 3457 STPY400 | 3602 SAW410 | -- |
|  |  | 3601 SAW410 |  |

Note (2):	Recognize lower minimum tensile or yield strengths of the underlined substitute materials in design consideration, or specify minimum tensile and yield strengths per ASTM.

STANDARD SPECIFICATION

| ASTM | JIS | BS | DIN |
| --- | --- | --- | --- |
| A-135 |  |  |  |
| Electric-Resistance-Welded |  |  |  |
| Steel Pipe |  |  |  |
| Gr A | G 3454 STPG370 (1) | 3601 ERW360 | 1626 St37.0 |
| Gr B | G 3454 STPG410 (1) | 3601 ERW410 | 1626 St44.0 . |
| A-139 |  |  |  |
| Electric-Fusion (Arc)-Welded |  |  |  |
| Steel Pipe (NPS 4 and over) |  |  |  |
| Gr A – E | G 3457 STPY400 (2)(3) | 3602 SAW410 (2) | --- |
|  |  | 3601 SAW410 (2) |  |
| A-211 |  |  |  |
| Spiral-Welded Steel or Iron Pipe |  |  |  |
| A 570 Gr 30-45 | G 357 STPY400 (2)(3) | 3602 SAW 410 (2) | --- |
|  |  | 3601 SAW 410 (2) |  |
| A 570 Gr 50 | --- | 3502 SAW 460 (2) |  |
| A-312 |  |  |  |
| Seamless and Welded Austenitic |  |  |  |
| Stainless Steel Pipe |  |  |  |
| TP 304 (18Cr-8Ni) | G 3459 SUS304TP | 3605-304S18,S25 | 17457/58 X5CrNi1810 |
| TP 304H (18Cr-8Ni) | G 3459 SUS304HTP | 3605-304S59 | --- |
| TP 304L (18Cr-8Ni) | G 3459 SUS304LTP | 3605-304S14,S22 | 17457/58 X2CrNi1911 |
| TP 309 (23Cr-12Ni) | G 3459 SUS309STP | --- | --- |
| TP 310 (25Cr-20Ni) | G 3459 SUS310STP | --- | --- |
| TP 316 (16Cr-12Ni-21Mo) | G 3459 SUS316TP | 3605-316S18,S26 | 17457/58 X5CrNiMo17122 |
| TP 316H (16Cr-12Ni-2Mo) | G 3459 SUS316HTP | 3605-316S59 | 17459E X6CrNiMo1713 |
| TP 316L (16Cr-12Ni-2Mo) | G 3459 SUS316LTP | 3605-316S14,S22 | 17457/58 X2CrNiMo17132 |
| TP 321 (18Cr-10Ni-Ti) | G 3459 SUS321TP | 3605-321S18,S22 | 17457/58 X6CrNiTi1810 |
| TP 321H (l8Cr-12Ni-Ti) | G 3459 SUS321HTP | 3605-321S59 | SEW470 X12CrNiTi189 |
| TP 347 (18Cr-10Ni-Cb) | G 3459 SUS347TP | 3605-347S18,S17 | 17457/58 X6CrNiNb1810 |
| TP 347H (18Cr-10Ni-Cb) | G 3459 SUS347H TP | 3605-347S59 | --- |

Note (1): 		Specify electric resistance-welding.

Note (2):	Recognize loner minimum tensile or yield strengths of the underlined substitute materials in design consideration, or specify minimum tensile and yield strengths per ASTM.

Note (3): 		Specify carbon, manganese, or silicon contents in accordance with ASTM.

STANDARD SPECIFICATION

| Note (1):Recognize Lower minimum tensile or yield strengths of the underlined substitute materials in design consideration or specify minimum tensile and yield strengths per ASTM. ASTM | JIS | BS | DIN |
| --- | --- | --- | --- |
| A-333 |  |  |  |
| Seamless and Welded Steel Pipe |  |  |  |
| for Low-Temperature Service |  |  |  |
| Gr 1 | G 3460 STPL380 | 3603-CFS410 LT50 | 17173 TTSt35N |
|  |  | 3603-HFS410 LT50 | 17174 TTSt35N |
|  |  | 3603-ERW410 LT50 |  |
|  |  | 3603-CEW410 LT50 |  |
| Gr 3 (3-1/2Ni) | G 3460 STPL450 | 3603-HFS503 LT100 | 17173 l0Ni14 |
|  |  | 3603-CFS503 LT100 |  |
| Gr 6 | --- | 3603-CFS410 LT50 | SEW680 TTSt45N |
|  |  | 3603-HFS410 LT50 |  |
|  |  | 3603-ERW410 LT50 |  |
|  |  | 3603-CEW410 LT50 |  |
| Gr 8 (9Ni) | G 3460 STPL690 | 3603-HFS509 LT196 | 17173 X8Ni9 |
|  |  | 3603-CFS509 LT196 |  |
| A-335 |  |  |  |
| Seamless Ferritic Alloy-Steel Pipe |  |  |  |
| for High-Temperature Service |  |  |  |
| Gr P1 (C-1/2Mo) | G 3458 STPA12 | --- | 17175 15Mo5 |
| Gr P5 (5Cr-1/2Mo) | G 3458 STPA25 | 3604 CFS625 (1) | Wbl 007/2 12CrMo195 (2) |
|  |  | 3604 HFS625 (1) |  |
| Gr P9 (9Cr-1Mo) | G 3458 STPA26 | 3604-CFS629-470 (1) | Wbl 109 X12CrMo91 (2) |
| Gr P11 (1-1/4Cr-1/2Mo) | G 3458 STPA23 | 3604 CF5621 | 17175 13CrMo44 |
|  |  | 3604 HFS621 |  |
| Gr P12 (1Cr-1/2Mo) | G 3458 STPA22 | 3604 CFS620-460 (1) | 17175 13CrMo44 |
|  |  | 3604 HFS620-460 (1) |  |
| Gr P22 (2-1/4Cr-1Mo) | G 3458 STPA24 | 3604 CFS622 | 17175 l0CrMo910 |
|  |  | 3604 HFS622 |  |

Note (2):VdTuv-Werkstoftblatt https://www.abtersteel.com/

STANDARD SPECIFICATION

| Note (1): Specify seamless. ASTM | JIS | BS |  | DIN |
| --- | --- | --- | --- | --- |
| A-358 |  |  |  |  |
| Electric-Fusion-welded Austenitic |  |  |  |  |
| Chromium-Nickel Alloy Steel Pipe |  |  |  |  |
| For High-Temperature Service |  |  |  |  |
| Grade Material |  |  |  |  |
| 304 A240, Type 304 | G 3468 SUS304TPY | 3605 LWHT 304S18 | 17457 | X5CrNi1810 |
| 304L A240, Type 304L | G 3468 SUS304LTPY | 3605 LWHT 304S14 | 17457 | X2CrNi1911 |
| 316 A240, Type 316 | G 3468 SUS316TPY | 3505 LWHT 316S18 | 17457 | X5CrNiMo17122 |
| 316L A240, Type 316L | G 3468 SUS316LTPY | 3605 LWHT 316S14 | 17457 | X2CrNiMo17132 |
| 321 A240, Type 321 | G 3468 SUS321TPY | 3605 LWHT 321S18 | 17457 | X6CrNiTi1810 |
| 347 A240, Type 347 | G 3468 SUS347TPY | 3605 LWHT 347S18 | 17457 | X6CrNiNb1810 |
| A-376 |  |  |  |  |
| Seamless Austenitic Steel Pipe for |  |  |  |  |
| High-Temperature Central-Station |  |  |  |  |
| Service |  |  |  |  |
| TP 304 (18Cr-8Ni) | G 3459 SUS304TP (1) | 3605-304S18 | 17459E | X6CrNi1811 |
| TP 304H (18Cr-8Ni) | G 3459 SUS304HTP (1) | 3605-304S59 |  | --- |
| TP 316 (16Cr-12Ni-2Mo) | G 3459 SUS316TP (1) | 3605-316S18 | 17458 | X5CrNiMo17122 |
| TP 316H (16Cr-12Ni-2Mo) | G 3459 SUS316HTP (1) | 3605-316S59 | 17459E | X6CrNiMo1713 |
| TP 321 (18Cr-10Ni-Ti) | G 3459 SUS321TP (1) | 3605-321S18 | 17458 | X6CrNiTi810 |
| TP 321H (18Cr-10Ni-Ti) | G 3459 SUS321HTP (1) | 3605-321S59 |  | --- |
| TP 347 (18Cr-10Ni-Cb) | G 3459 SUS347TP (1) | 3605-347S18 | 17458 | X6CrNiNb1810 |
| TP 347H (18Cr-10Ni-Cb) | G 3459 SUS347HTP (1) | 3605-347S59 |  | --- |
| A-409 Welded Large Diameter Austenitic |  |  |  |  |
| Steel Pipe for Corrosive or High |  |  |  |  |
| Temperature Service |  |  |  |  |
| TP 304 (18Cr-8Ni) | G 3468 SUS304TPY | --- | 17457 | X5CrNi810 |
| TP 304L | G 3463 SUS304LTPY | --- | 17457 | X2CrNi1911 |
| TP 316 (16Cr-12Ni-2Mo) | G 3468 SUS316TPY | --- | 17457 | X5CrNiMo17122 |
| TP 316L | G 3468 SUS316LTPY | --- | 17457 | X2CrNiMo17132 |
| TP 321 (18Cr-10Ni-Ti) | G 3468 SUS321TPY | --- | 17457 | X6CrNiTi1810 |
| TP 347 (18Cr-10Ni-Cb) | G 3468 SUS347TPY | --- | 17457 | X6CrN iNb1810 |

STANDARD SPECIFICATION

| Note (i): Specify electric resistance-welding. ASTM | JIS/JPI | BS | DIN |
| --- | --- | --- | --- |
| A-524 |  |  |  |
| Seamless Carbon Steel Pipe for |  |  |  |
| Atmospheric and Lower |  |  |  |
| Temperatures |  |  |  |
| Gr 1 | --- | --- | SEW680 TTSt41 |
| Gr 11 |  |  | --- |
| A-587 |  |  |  |
| Electric-Welded Low-Carbon |  |  |  |
| Steel Pipe for the Chemical |  |  |  |
| Industry |  |  |  |
|  | G 3454 STPG370 (1)(2) | --- | 1626 St37.0 |
| A-671 |  |  |  |
| Electric-Fusion-Welded Steel pipe |  |  |  |
| for Atmospheric and Lower |  |  |  |
| Temperatures |  |  |  |
| Grade Material |  |  |  |
| CA55 A285 Gr C |  |  |  |
| CB60 A515 Gr 60 | JPI-SB42 | --- | --- |
| CB70 A515 Gr 65 | JPI-SB46 | --- | --- |
| CB70 A515 Gr 70 | JPI-SB49 | --- | --- |
| CC60 A516 Gr 60 | JPI-SLA24B (3) | --- | --- |
| CC65 A516 Gr 65 | JPI-SLA33B (3) | --- | --- |
| CD70 A537 CL 1 | --- | --- | --- |
| CE55 A442 Gr 55 | --- | --- | --- |
| CE60 A442 Gr 60 | JPI-SPV24 | --- | --- |
| CF70 A203 Gr B | --- | --- | --- |
| CF71 A203 Gr E | JPI-SL3N28 | --- | --- |
| CK75 A299 |  |  |  |

Note (2): 	Maximum carbon content shall be 0.15%.

Note (3): 	Specify Impact Test requirement per ASTM.

STANDARD SPECIFICATION

| Note (1): Specify Impact Test requirement per ASTM. ASTM | JIS/JPI | BS | DIN |
| --- | --- | --- | --- |
| A-672 |  |  |  |
| Electric-Fusion-Welded Steel Pipe |  |  |  |
| for High- Pressure Service at |  |  |  |
| Moderate Temperature |  |  |  |
| Grade Material |  |  |  |
| A55 A285 Gr C | JPI-SB42 | --- | --- |
| B55 A515 Gr 55 | --- | --- | --- |
| B60 A515 Gr 60 | JPI-SB42 | --- | --- |
| B65 A515 Gr 65 | JPI-SB46 | --- | --- |
| B70 A515 Gr 70 | JPI-SB49 | --- | --- |
| C55 A516 Gr 55 | --- | --- | --- |
| C60 A516 Gr 60 | JPI-SLA24B (1) | --- | --- |
| C65 A516 Gr 65 | JPI-SLA33B (1) | --- | --- |
| C70 A516 Gr 70 | --- | --- | --- |
| D70 A537 CL 1 | --- | --- | --- |
| E55 A442 Gr 55 | --- | --- | --- |
| E60 A442 Gr 60 | JPI-SPV24 | --- | --- |
| L65 A204 Gr A | JPI-SB46M | --- | --- |
| L70 A204 Gr B | JPI-SB49M (2) |  |  |
| L75 A204 Gr C | --- | --- | --- |
| N75 A299 | --- | --- | --- |

Note (2):	Recognize loner minimum tensile or yield strengths of the underlined substitute materials in design consideration, or specify minimum tensile and yield strengths per ASTM.

STANDARD SPECIFICATION

| ASTM/API | JIS/JPI | BS | DIN |
| --- | --- | --- | --- |
| A-691 |  |  |  |
| Carbon and Alloy Steel Pipe, |  |  |  |
| Electric-Fusion-Welded for |  |  |  |
| High- Pressure Service |  |  |  |
| at High Temperatures |  |  |  |
| Grade Material |  |  |  |
| CM-65 A204 Gr A | JPI-SB46M | --- | --- |
| CM-70 A204 Gr B | JPI-SB49M | --- | --- |
| CM-75 A204 Gr C | --- | --- | --- |
| CMSH-70 A537 CL 1 | --- | --- | --- |
| CMS-75 A299 | --- | --- | _-- |
| ½ Cr A337 Gr 2 CL 1 | --- | --- | --- |
| 1 Cr A387 Gr 12 CL 1 | JPI-SCMV2 | --- | --- |
| 1-1/4 Cr A387 Gr 11 CL1 | JPI-SCMV3 | --- | --- |
| 2-1/4 Cr A387 Gr 22 CL1 | JPI-SCMV4 | --- | --- |
| 5 Cr A387 Gr 5 CL 1 | JPI-SCMV6 | --- | --- |
| API 5L |  |  |  |
| Line Pipe |  |  |  |
| Gr A25 | 63452 SGP | 1387 | --- |
| Gr A | 63454 STPG370 | 3601 ERW 360 | 17172 StE210.7 |
|  |  | 3601 S 360 |  |
| Gr B | 63454 STPG410 | 3601 ERW 430 (1) | 17172 StE240.7 |
|  |  | 3601 S 430 (1) |  |
|  |  | 3601 SAW 430 (1) |  |
|  |  | 6327 Part 1-8 (1) |  |
| Gr X42 | --- | --- | 17172 StE290.7 |
| Gr X46 | --- | --- | 17172 StE320.7 |
| Gr X52 | --- | --- | 17172 StE360.7 |
| Gr X56 | --- | --- | 17172 StE385.7 |
| Gr X60 | --- | --- | 17172 StE415.7 |
| Gr X65 | --- | --- | 17172 StE445.7TM |
| Gr X70 | --- | --- | 17172 StE480.7TM |
| --- | 63455 STS370 | --- | 1630 St37.4 |
| --- | 63455 STS410 | --- | 1630 St44.4 |
| --- | 63455 STS480 | --- | 1630 St52.4 |

Note (1):	Recognize lower minimum tensile or yield strengths of the underlined substitute materials in design consideration, or specify minimum tensile and yield strengths per ASTM.

Table 3 TUBES

| ASTM | JIS | BS | DIN |
| --- | --- | --- | --- |
| A-161 |  |  |  |
| Seamless Low-Carbon and Carbon |  |  |  |
| Molybdenum Steel Still Tubes for |  |  |  |
| Refinery Service Low Carbon Steel |  |  |  |
|  | G 3461 ST340 (1) (2) | 3059 HFS320 (2) | 17175 St35.8 |
|  |  | 3059 CFS320 (2) |  |
| Gr T1 | G 3462 STBA12 (1)(2)(3) | --- | 17175 15Mo5 |
|  | G 3467 STFA12 (2) |  |  |
| A-178 |  |  |  |
| Electric-Resistance-Welded Carbon Steel and |  |  |  |
| Carbon-Manganese Steel |  |  |  |
| Boiler Tubes |  |  |  |
| Gr A | G 3461 STB340 (40 | 3059 ERW320 (3) | 17177 St37.8 |
|  |  | 3059 CEW320 (3) |  |
| Gr C | G 3461 STB410 (4) | 3059 ERW360 | 17177 St42.8 |
|  |  | 3059 CEW360 (3) |  |
| Gr D | --- | 3059 ERW440 (3) | --- |
|  |  | 3059 CEW440 (3) |  |
| A-179 |  |  |  |
| Seamless Cold-Drawn Low-Carbon |  |  |  |
| Steel Heat-Exchanger and Condenser Tubes |  |  |  |
|  | G 3461 STB340 (1)(5)(6) | 3606 CFS 320 | 17175 St35.8 |
|  |  | 3059 S1 360 (5)(6) |  |

Note (1): Specify seamless.

Note (2): Maximum hardness shall be as follows:

| Item | Carbon Steel | Gr T1 |
| --- | --- | --- |
| Hot rolled tubes Cold drawn tubes | HB 137 HB 125 | HB 150 HB 137 |

Note (3): Specify killed steel.

Note (4): Specify electric resistance-welding.

Note (5): Specify cold drawn.

Note (6): Maximum hardness shall be Rockwell B72.

STANDARD SPECIFICATION

| ASTM | JIS | BS | DIN |
| --- | --- | --- | --- |
| A-192 |  |  |  |
| Seamless Carbon Steel Boiler |  |  |  |
| Tubes for High- Pressure Service |  |  |  |
|  | G 3-061 STB340 (1)(2) | 3059 HFS 320 (2) | 17175 St35.8 |
|  |  | 3059 CFS 320 (2) |  |
|  |  | 3059 S1 360 (2) |  |
|  |  | 3059 S2 360 (2) |  |
| A-199 |  |  |  |
| Seamless Cold-Drawn Intermediate |  |  |  |
| Alloy-Steel Heat-Exchenger and |  |  |  |
| Condenser Tubes |  |  |  |
| Gr T5 | G 3462 STBA25 (3)(4) | 3606 CFS 625 | Wbl 007/2 12CrMio195 (6) |
| Gr T9 | G 3462 STBA26 (3)(5) | 3059 S1 629-470 (3)(5) | Wbl 109 X12CrMo91 (6) |
|  |  | 3059 S2 629-470 (3)(5) |  |
| Gr T11 | G 3462 STBA23 (3)(4) | 3606 CFS621 | 17175 13CrMo44 |
| Gr T22 | G 3462 STBA24 (3)(4) | 3606 CFS622 | 17175 10CrMo910 |
|  |  | 3059 S1 622-440 (3)(4) |  |
|  |  | 3059 S2 622-440 (3)(4) |  |
| A-200 |  |  |  |
| Seamless Intermediate Alloy-Steel |  |  |  |
| Still Tubs for Refinery Service |  |  |  |
| Gr T5 | G 3462 STBA25 (4) | 3604 CFS625 (4) | Wbl 007/2 12CrMo195 (6) |
|  | G 3467 STFA25 (4) | 3604 HFS625 (4) |  |
| Gr T7 | --- | --- | --- |
| Gr T9 | G 3462 STBA26 (5) | 3604 CFS629-470 (5) | Wbl 109 X12CrMo91 (6) |
|  | G 3467 STFA26 (5) | 3604 HFS629-470 (5) |  |
|  |  | 3059 S1 629-470 (5) |  |
|  |  | 3059 S2 629-470 (5) |  |
| Gr T11 | G 3462 STBA23 (4) | 3604 CFS621 (4) | 17175 13CrMo44 |
|  | G 3467 STFA23 (4) | 3604 HES621 (4) |  |
| Gr T22 | G 3462 STBA24 (4) | 3059 S1 622-440 (4) | 17175 10CrMo910 |
|  | G 3467 STFA24 (4) | 3604 CFS622 (4) |  |
|  |  | 3604 HFS622 (4) |  |

Note (1): Specify seamless.

Note (2): Maximum hardness shall be Rockwell 677.

Note (3): Specify cold drawn.

Note (4): Maximum hardness shall be Rockwell 885.

Note (5): Maximum hardness shall be Rockwell B89.

Note (6): VdTuv-Herkstoftblatt

STANDARD SPECIFICATION

| ASTM | JIS | BS | DIN |
| --- | --- | --- | --- |
| A-209 |  |  |  |
| Seamless Carbon-Molybdenum |  |  |  |
| Alloy-Steel Boiler and Super |  |  |  |
| Heater Tubes |  |  |  |
| Gr T1 | G 3462 STBA12 (1)(2) | 3059 S1 243 (2) | 17175 15Mo5 |
|  |  | 3059 S2 243 (2) | --- |
| Gr Tla | G 3462 STBA13 (1)(3) | 3059 S1 243 (3) | 17175 15Mo5 |
|  |  | 3059 S2 243 (3) | ~ |
| Gr Tlb | --- | --- | --- |
| A-210 |  |  |  |
| Seamless Medium-Carbon Steel |  |  |  |
| Boiler and Super heater Tubes |  |  |  |
| Gr A1 | G 3461 STB410 (1)(4) | 3059 S1 440 | 17175 St45.8 |
|  |  | S2 440 (4) |  |
| A-213 |  |  |  |
| Seamless Ferritic and Austenitic |  |  |  |
| Alloy-Steel Boiler, Super heater |  |  |  |
| and Heat-Exchanger Tubes |  |  |  |
| Gr T 5 | G 3462 STBA25 (5) | 3606 CFS 625 | Wbl 007/2 12CrMo195 (7) |
| Gr T 11 | G 3462 STBA23 (5) | 3606 CFS 621 | 17175 13CrMo44 |
| Gr T 12 | G 3462 STBA22 (1)(5) | 3506 CFS 620 | 17175 13CrMo44 |
|  |  | 3059 S1/S2 620 (5) |  |
| Gr T 22 | G 3462 STBA24 (5) | 3606 CFS 622 | 17175 10CrMo910 |
|  |  | 3059 S1/S2622-440/490(5) |  |
| Gr TP 304 | G 3463 SUS304 TB (1)(6) | 3606 CFS 304S25 | 17458 X5CrNi1810 |
| Gr TP 3D4H | G 3463 SUS304H T8 (1)(6) | 3059 CFS304S59 (6) | --- |
| Gr TP 304L | G 3463 SUS304L TB (1)(6) | 3606 CFS304S22 | 17458 X2CrNi1911 |
| Gr TP 310 | G 3463 SUS310S TB (1)(6) | --- | --- |
| Gr TP 316 | G 3463 SUS316 TB (1)(6) | 3606 CFS316S25 | 17458 X5CrNiMo17122 |
| Gr TP 316H | G 3463 SUS316H TB(1)(6) | 3059 CFS316S59 (6) | 17459E X6CrNiMo1713 |
| Gr TP 316L | G 3463 SUS316L TB (1)(6) | 3606 CFS316S29 | 17458 X2CrNiMo17132 |
| Gr TP 321 | G 3463 SUS321 TB (1)(6) | 3606 CF5321S22 | 17458 X6CrNiTi1810 |
| Gr TP 321H | G 3463 SUS321H TB(1)(6) | 3059 CFS321S59 (6) | --- |
| Gr TP 347 | G 3463 SUS347 TB (1)(6) | 3606 CFS347S17 | 17458 X6CrNiNb1810 |
| Gr TP 347H | G 3463 SUS347H TB(1)(6) | 3059 CFS347S59 (6) | --- |

Note (1): Specify seamless.

Note (2): Maximum hardness shall be Rockwell B90.

Note (3): Maximum hardness shall be Rockwell B81.

Note (4): Maximum hardness shall be Rockwell B79.

Note (5): Maximum hardness shall be Rockwell B85.

Note (6): Maximum hardness shall be Rockwell B90.

Note (7): VdTuv-Werkstoftblatt

STANDARD SPECIFICATION

| ASTM | JIS | BS | DIN |
| --- | --- | --- | --- |
| A-214 |  |  |  |
| Electric-Resistance-Welded |  |  |  |
| Carbon Steel Heat-Exchanger |  |  |  |
| and Condenser Tubes |  |  |  |
|  | G 3461 STB340 (1)(2) | 3606 ERW 320 | 17177 St37.8 |
|  |  | 3059 ERW 320 (2) |  |
|  |  | 3059 CEW 320 (2) |  |
|  |  | 3059 ERW 360 (2) |  |
|  |  | 3059 CEW 360 (2) |  |
| A-226 |  |  |  |
| Electric-Resistance-Welded |  |  |  |
| Carbon Steal Boiler and |  |  |  |
| Superheater Tubes for |  |  |  |
| High-Pressure Service |  |  |  |
|  | G 3461 STB340 (1)(2) | 3059 ERW320 (2) | 17177 St37.8 |
|  |  | 3059 CEW320 (2) |  |
|  |  | 3059 ERW360 (2) |  |
|  |  | 3059 CEW360 (2) |  |
| A-249 |  |  |  |
| Welded Austenitic Steel Boiler, |  |  |  |
| Superheater, Heat-Exchanger, |  |  |  |
| and Condense; Tubes |  |  |  |
| TP 304 | G 3463 SUS304 TB (3) | --- | 17457 X5CrNi1810 |
| TP 304H | G 3463 SUS304H TB (3) | 3059-ERW304S59 (3) | --- |
| TP 304L | G 3463 SUS304L TB (3) | --- | 17457 X2CrNi1911 |
| TP 309 | G 3463 SUS309S TB (3) | --- | --- |
| TP 310 | G 3463 SUS310S TB (3) | --- | --- |
| TP 316 | G 3463 SUS316 TB (3) | --- | 17457 X5CrNiMo17122 |
| TP 316H | G 3463 SUS316H TB (3) | 3059-ERW316S59 (3) |  |
| TP 316L | G 3463 SUS316L TB (3) | --- | 17457 X2CrNiMo17132 |
| TP 321 | G 3463 SUS321 TB (3) | --- | 17457 X6CrNiTi1810 |
| TP 321H | G 3463 SUS321H TB (3) | 3059 ERW321S59 (3) | --- |
| TP 347 | G 3463 SUS347 TB (3) | --- | 17457 X6CrNiNb1810 |
| TP 347H | G 3463 SUS347H TB (3) | 3059-ERW347S59 (3) | --- |

Note (1): Specify electric resistance-welding.

Note (2): Maximum hardness shall be Rockwell B72.

Note (3): Maximum hardness shall be Rockwell B90.

STANDARD SPECIFICATION

| ASTM | JIS | BS | DIN |
| --- | --- | --- | --- |
| A-268 |  |  |  |
| Seamless and Welded Ferritic |  |  |  |
| Stainless Steel Tubing for |  |  |  |
| General Service |  |  |  |
| TP 410 | G 3463 SUS410 TB (1) | --- | --- |
| TP 430 | G 3463 SUS430 TB (2) | --- | --- |
| A-269 |  |  |  |
| Seamless and Welded Austenitic |  |  |  |
| Stainless Steel Tubing for |  |  |  |
| General Service |  |  |  |
| TP 304 | G 3463 SUS304 TB (2) | 3605-304S18,S25 (2) | --- |
| TP 304L | G 3463 SUS304L TB (2) | 3605-304S14,S22 (2) | --- |
| TP 316 | G 3463 SUS316 TB (2) | 3605-316S18,S26 (2) | --- |
| TP 316L | G 3463 SUS316L TB (2) | 3605-316S14,S22 (2) | --- |
| TP 321 | G 3463 SUS321 TB (2) | 3605-321S18,S22 (2) | --- |
| TP 347 | G 3463 SUS347 TB (2) | 3605-347S18,S17 (2) | --- |
| A-271 |  |  |  |
| Seamless Austenitic Chromium |  |  |  |
| Nickel Steal Still Tubes for |  |  |  |
| Refinery Service |  |  |  |
| TP 304 | G 3463 SUS304 TB (2)(3) | 3605-304S18 (2) | 17459E X6CrNi1811 |
|  | G 3467 SUS304 TF (2) |  |  |
| TP 304H | G 3463 SUS304H TB (2)(3) | 3605-304S59 (2) | --- |
|  | G 3467 SUS304H TF (2) | 3059-CFS304S59 (2) |  |
| TP 316 | G 3463 SUS316 TB (2)(3) | 3605-316S18 (4) | 17458 X5CrNiMo17122 |
|  | G 3467 SUS316 TF (2) |  |  |
| TP 316H | G 3463 SUS316 HTB (2)(3) | 3605-316S59 (4) | 17459E X6rNiMo1713 |
|  | G 3467 SUS316 HTF (2) | 3059-316S59 (4) |  |
| TP 321 | G 3463 SUS321 TB (2)(3) | 3605-321S18 (2) | 17458 X6CrNiTi1810 |
|  | G 3467 SUS321 TF (2) |  |  |
| TP 321H | G 3463 SUS32114 TB (2)(3) | 3605-321S59 Gr 1010 (2) | --- |
|  | G 3467 SUS321H TF (2) | 3059-CFS321S59 Gr 1010(2) |  |
| TP 347 | G 3463 SUS347 TB (2)(3) | 3605-347S18 (2) | 17458 X6CrNiNb1810 |
|  | G 3467 SUS347 TF (2) |  |  |
| TP 347H | G 3463 SUS347H TB (2)(3) | 3605-347S59 (2) | --- |
|  | G 3467 SUS347H TF (2) | 3059-CFS347S59 (2) | --- |

Note (1): Maximum hardness shall be Rockwell B95.

Note (2): Maximum hardness shall be Rockwell B90.

Note (3): Specify seamless.

Note (4): Maximum carbon content shall be 0.21%

STANDARD SPECIFICATION

| ASTM | JIS | BS | DIN |
| --- | --- | --- | --- |
| A334 |  |  |  |
| Seamless and Welded Carbon |  |  |  |
| And Alloy-Steel Tubes for |  |  |  |
| Low-Temperature Service |  |  |  |
| Gr 1 | G 3464 STBL380 (1) | 3603 CEW410 LT50 (1) | 17173 T7St35N |
|  |  | 3603 CFS410 LT50 (1) | 17174 TTSt35N |
|  |  | 3603 ERW410 LT50 (1) |  |
|  |  | 3603 HFS410 LT50 (1) |  |
| Gr 3 | G 3464 STBL450 (2) | 3603 CFS503 LT100 (2) | 17173 10Ni14 |
|  |  | 3603 HFS503 LT100 (2) |  |
| Gr 6 | --- | 3603 CEW410 LT50 (2) | SEW680 TTSt45N |
|  |  | 3603 CFS410 LT50 (2) |  |
|  |  | 3603 ERW410 LT50 (2) |  |
|  |  | 3603 HFS4110 LT50 (2) |  |
| Gr 8 | G 3464 STBL690 (2) | 3603 CFS509 LT196 (2) | 17173 X8Ni9 |
|  |  | 3603 HFS509 LT196 (2) |  |

Note (1): Maximum hardness shall be Rockwell B85.

Note (2): Maximum hardness shall be Rockwell B90.

STANDARD SPECIFICATION

Table 4 FORGINGS

| ASTM | JIS | BS | DIN |
| --- | --- | --- | --- |
| A-105 |  |  |  |
| Forging, Carbon Steel, |  |  |  |
| For Piping Components |  |  |  |
|  | G 3202 SFVC2A | 1503-221-490 | --- |
| A-181 |  |  |  |
| Forging, Carbon Steel, for |  |  |  |
| General - Purpose Piping |  |  |  |
| Class 60 | G 3202 SFVC1 | 1503-221-430 | 17200 C22N |
| Class 70 | G 3202 SFVC2A | 1503-221-490 | --- |
| A-182 |  |  |  |
| Forged or Rolled Alloy-Steel |  |  |  |
| Pipe Flanges, Forged Fittings, |  |  |  |
| and Valves and Parts for |  |  |  |
| High –Temperature Service |  |  |  |
| F1 (C-1/2Mo) | G 3203 SFVAF1 | 1503-245-420 (1) | VdTuv201 16Mo5 |
| FS (5Cr-1/2Mo) | G 3203 SFAF58 | 1503-625-520 | VdTuv1207 12CrMo195 |
| F9 (9Cr-1Mo) | G 3203 SFVAF9 | --- | W.St.Nr17386 X12CrMo910 |
| F11 (1-1/4Cr-I/2Mo) | G 3203 SFVAF11A | 1503-621-460 | SEW550 16CrMo44 |
| F12 (1Cr-1/2Mo) | G 3203 SFVAF12 | 1503-620-540 | SEW550 13CrMo44 |
| F21 (3Cr-1Mo) | G 3203 SFVAF21B | --- | --- |
| F22 (2-1/4Cr-1Mo) | G 3203 SFVAF22B | 1503-622-560 | SEW550 10CrMo9I0 |
| F304 (18Cr-8Ni) | G 3214 SUS304 | 1503-304S31 | 17440 X5CrNi1810 |
| F304H (18Cr-8Ni) | G 3214 SUS304H | 1503-304S51 | --- |
| F304L (18Cr-8Ni) | G 3214 SUSF304L | 1503-304S11 | 17440 X2CrNi1911 |
| F316 (16Cr-12Ni-2Mo) | G 3214 SUSF316 | 1503-316S31 or 33 | 17440 X5CrNiMo17122 |
| F316H (16Cr-12Ni-2Mo) | G 3214 SUSF316H | 1503-316S51 | --- |
| F316L (16Cr-12Ni-2Mo) | G 3214 SUS316L | 1503-316S11 or 13 | 17440 X2CrNiMo17132 |
| F321 (18Cr-10Ni-Ti) | G 3214 SUS321 | 1503-321S31 | 17440 X6CrNiTi1810 |
| F321H (18Cr-10Ni-Ti) | G 3214 SUSF321H | 1503-321S51-510 | --- |
| F347 (18Cr-10Ni-Cb) | G 3214 SUSF347 | 1503-347S31 | 17440 X6CrNiNb1810 |
| F347H (18Cr-10Ni-Cb) | G 3214 SUSF347H | 1503-347S51 | --- |

Note (1):	Recognize lower minimum tensile or yield strengths of the underlined substitute materials in design consideration, or specify minimum tensile and yield strengths per ASTM.

STANDARD SPECIFICATION

| ASTM | JIS | BS | DIN |
| --- | --- | --- | --- |
| A-226 |  |  |  |
| Forging, Carbon Steel, for |  |  |  |
| Pressure Vessel Component |  |  |  |
| Class 1 | G 3202 SFVC1 | 1503-221-430 | 17200 C22N |
| Class 2 | G 3202 SFVC2A | 1503-221-490 | --- |
| Class 4 | G 3202 SFVC2B |  |  |
| A-336 |  |  |  |
| Steel Forging, Alloy, for Pressure | Refer to A-182 | Refer to A-182 | Refer to A-182 |
| and High- Temperature Parts |  |  |  |
| A-350 |  |  |  |
| Forging, Carbon and Low-Alloy |  |  |  |
| Steel, Requiring Notch Toughness |  |  |  |
| Testing for Piping Component |  |  |  |
| LF1 | G 3205 SFL1 | 1503-221-430 (1) | SEW680 TTSt41 |
| LF2 | G 3205 SFL2 | 1640 WPLO | SEW680 TTStE36 |
|  |  | 1503-221-490 (1) |  |
| LF3 (3-1/2Ni) | G 3205 SFL3 | 1640 WPL3 | 17280 10Ni14 |
|  |  | 1503-503-490 (1) |  |
| A-508 |  |  |  |
| Quenched and Tempered |  |  |  |
| Vacuum-Treated Carbon and Alloy |  |  |  |
| Steel Forging for Pressure Vessel |  |  |  |
| Class 1 | G 3202 SFVC2B | --- | --- |
| Class 2 | G 3204 SFVQ2A | --- | SEW640 22NiMoCr37 |
| Class 3 | G 3204 SFVQ1A | --- | SEW640 20MrMoNi55 |
| A-541 |  |  |  |
| Steel Forging, Carbon and Alloy |  |  |  |
| Quenched and Tempered, for |  |  |  |
| Pressure Vessel Component |  |  |  |
| Class 1 | G 3202 SFVC2B | 1503-221-490 (1)(2) | --- |
| Class 2 | G 3204 SFVQ2A | --- | --- |
| Class 3 | G 3204 SFVQ1A | --- | --- |

Note (1): Specify Impact Test requirement per ASTM.

Note (2): Specify heat treatment and mechanical properties per ASTM.

STANDARD SPECIFICATION

Table 5 CASTINGS

| ASTM | JIS | BS | DIN |
| --- | --- | --- | --- |
| A-27 |  |  |  |
| Steel Castings, Carbon, for |  |  |  |
| General Application |  |  |  |
| Gr 60-30 | G 5101 SC410 (1) | 3100 Steel A1 | 1681 GS-38 (2) |
| Gr 65-35 | G 5101 SC450 (1) | --- | 1681 GS-45 |
| Gr 70-36 | G 5101 SC480 (1) | 3100 Steel A2 | 1681 GS-52 |
| A-47 |  |  |  |
| Ferrltic Malleable Iron Castings |  |  |  |
| Gr 32510 | G 5702 FCM3340 | 6681 B35-12 | 1692 GTS-35-10 |
| Gr 35018 | G 5702 FCM3360 | --- | 1692 GTS-35-10 (2) |
| A-48 |  |  |  |
| Gray Iron Castings |  |  |  |
| Class 20 | G 5501 FC150 | 1452 Gr 150 | 1691 GG-15 |
| Class 25 | G 5501 FC200 | 1452 Gr 180 | 1691 GG-20 |
| Class 30 | G 5501 FC200 (2) | 1452 Gr 220 | 1691 GG-20 (2) |
| Class 35 | G 5501 F 250 | 1452 Gr 260 | 1691 GG-25 |
| Class 40 | G 5501 FC300 | 1452 Gr 300 | 1691 GG-30 |
| Class 45 | G 5501 FC300 (2) | 1452 Gr 300 (2) | 1691 GG-30 (2) |
| Class 50 | G 5501 FC350 | 1452 Gr 350 | 1691 GG-35 |
| Class 55 | --- | 1452 Gr 400 | --- |
| Class 60 | --- | --- |  |
| A-126 |  |  |  |
| Gray Iron Castings for Valves |  |  |  |
| Flanges and Pipe Fittings |  |  |  |
| Class A | G 5501 FC200 | 1452 Gr 180 | 1691 GG-15 |
| Class 6 | G 5501 FC250 | 1452 Gr 260 | 1691 GG-25 |
| Class C | G 5501 FC300 | 1452 Gr 300 | 1691 GG-30 |

Note (1): Specify carbon, manganese, or silicon contents in accordance with ASTM.

Note (2):	Recognize lower minimum tensile or yield strengths of the underlined substitute materials in design consideration, or specify minimum tensile and yield strengths per ASTM.

STANDARD SPECIFICATION

| ASTM | JIS | BS | DIN |
| --- | --- | --- | --- |
| A-216 |  |  |  |
| Steel Castings, Carbon, |  |  |  |
| Suitable for Fusion Welding, |  |  |  |
| For High-Temperature Service |  |  |  |
| WCA | G 5151 SCPH1 (1) | 1504-161 Gr 430 | 17245 GS-C25 |
| WCB | G 5151 SCPH2 (1) | 1504-161 Gr 480 | 17245 GS-C25 |
| WCC | --- | 1504-161 Gr 540 (2)(3) | --- |
| A-217 |  |  |  |
| Steel Castings, Martensitic |  |  |  |
| Stainless and Alloy, for |  |  |  |
| Pressure-Containing Parts, |  |  |  |
| Suitable for High-Temperature |  |  |  |
| Service |  |  |  |
| WC1 (C-1/2Mo) | G 5151 SCPH11 (1) | 1504-245 | 17245 GS-22Mo4 |
| WC6 (1-1/4Cr-1/2Mo) | G 5151 SCPH21 (1) | 1504-621 | 17245 GG-17CrMo55 |
| WC9 (2-1/4Cr-1Mo) | G 5151 SCPH32 (1) | 1504-622 | 17245 CS-19CrMo910 |
| C5 (Cr-1/2Ho) | G 5151 SCPH61 (1) | 1504-625 | SEW 595 GS-2CrMo195 |
| C12 (9Cr-1Mo) | --- | 1504-629 | SEW 595 GS-2CrMo101 |
| A-297 |  |  |  |
| Steel Castings, Iron-Chromium |  |  |  |
| and Iron-Chromium-Nickel, Heat |  |  |  |
| Resistant, for General Application |  |  |  |
| Gr HC | G 5122 SCH2 | --- | --- |
| Gr HD | G 5122 SCH11 | --- | --- |
| Gr HE | G 5122 SCH17 | 3100-309C40 | --- |
| Gr HF | G 5122 SCH12 | 3100-302C35 | --- |
| Gr HH | G 5122 SCH13 | 3100-309C30 | --- |
| Gr HI | G 5122 SCH18 | --- | --- |
| Gr HK | G 5122 SCH22 or 21 | 3100-310C40 | --- |
| Gr HN | G 5122 SCH19 | 3100-311C11 | --- |
| Gr HT | G 5122 SCH15 | 3100-330C12 | --- |
| Gr HU | G 5122 SCH20 | 3100-331C60 | --- |

Note (1):Test and inspect the product in accordance with ASTH, except for the chemical analysis and mechanical properties of the steel.

Note (2): Specify carbon, manganese, or silicon contents in accordance with ASTM.

Note (3): Specify elongation in accordance with ASTM.

STANDARD SPECIFICATION

| ASTM | JIS | BS | DIN |
| --- | --- | --- | --- |
| A-338 |  |  |  |
| Malleable Iron Flanges, Pipe |  |  |  |
| Fittings, and Valve Parts for |  |  |  |
| Railroad, Marine, and Other |  |  |  |
| Heavy Duty Service at |  |  |  |
| Temperatures up to 650°F |  |  |  |
| (345°C) |  |  |  |
| A-351 |  |  |  |
| Steel Castings, Austenitic, |  |  |  |
| for High-Temperature Service |  |  |  |
| Gr CF3 (18Cr-8Ni) | G 5121 SCS19A (1) | 1504-304C12 (2) | --- |
|  |  | 3100-304C12 (2) |  |
| Gr CF3A (18Cr-8Ni) | --- | --- | --- |
| Gr CF3M (17Cr-10Ni-2Mo) | G 5121 SCS16A (1) | 1504-316C12 (2) | --- |
|  |  | 3100-316C12 (2) |  |
| Gr CF8 (18Cr-8Ni) | G 5121 SCS13A (1) | 1504-304C15 | 17445 G-X6CrNi189 |
|  |  | 3100-304C15 |  |
| Gr CF8A (18Cr-8Ni) | --- | --- | _-- |
| Gr CF8C (20Cr-10Ni-Cb) | G 5121 SCS21 (1) | 1504-347C17 | 17445 G-X5CrNiNb189 |
|  |  | 3100-347C17 |  |
| Gr CF8M (18Cr-10Ni-2Mo) | G 5121 SCS14A (1) | 1504-316C16 | 17445 G-X6CrNiMo1810 |
|  |  | 3100-316C16 |  |
| Gr CH10 (25Cr-13Ni) | G 5121 SCS17 (1)(2) | --- | --- |
| Gr CH20 (25Cr-13Ni) | G 5121 SCS17 (1)(3) | 3100-309C30 | --- |
| Gr CK20 (25Cr-20Ni) | G 5121 SCS18 (1) | --- | --- |
| Gr CN7M (28Ni-20Cr- | G 5121 SCS23 (1) | 1504-332C11 | --- |
| 2Mo-3Cb) |  |  |  |
| Gr HK40 (25Cr-20Ni) | G 5122 SCH22 (1) | 1504-310C40 | --- |
|  |  | 3100-310C40 |  |

Note (1):	Test and inspect the product in accordance with ASTM, except for the chemical analysis and mechanical properties of the steel.

Note (2):	Recognize lower minimum tensile or yield strengths of the underlined substitute materials in design consideration, or specify minimum tensile and yield strengths per ASTM.

Note (3): Specify mechanical properties, test and inspection in accordance with ASTM.

STANDARD SPECIFICATION

| ASTM | JIS | BS | DIN |
| --- | --- | --- | --- |
| A-352 |  |  |  |
| Steel Castings, Ferritic and |  |  |  |
| Martensitic, for Pressure- |  |  |  |
| Containing Parts Suitable for |  |  |  |
| Low-Temperature Service |  |  |  |
| LCB | G 5152 SCPL1 (1) | 1504-161 Gr 480 LT40 | SEW685 GS-CK24 |
| LC1 (C-1/2Mo) | G 5152 SCPL11 (1) | 1504-245 LT50 | --- |
|  |  | 3100-BL1 |  |
| LC2 (2-1/2Ni) | G 5152 SCPL21 (1) | --- | --- |
| LC3 (3-1/2Ni) | G 5152 SCPL31 (1) | 1504-503 LT60 | SEW685 GS-10Ni14 |
|  |  | 3100-BL2 |  |
| LC9 | --- | --- | --- |
| A-395 |  |  |  |
| Ferritic Ductile Iron Pressure- |  |  |  |
| Retaining Castings for Use at |  |  |  |
| Elevated Temperatures |  |  |  |
|  | 88243, APPENDIX-1 | 2789 Gr 420/12 (2) | --- |
|  | FCD-S |  |  |
| A-447 |  |  |  |
| Steel Castings, Chromium-Nickel |  |  |  |
| -Iron Alloy Castings (25-12 Class) |  |  |  |
| for High-Temperature Service |  |  |  |
|  | G 5122 SCH13 (3) | 3100-309C32 | --- |
| A-494 |  |  |  |
| Casting, Nickel and Nickel Alloy |  |  |  |
| M-35-1 | --- | 3071-NAI | --- |
| M-30H | --- | 3071-NA2 (4) | --- |
| M-25S | --- | 3071-NA3 | --- |

Note (1):	Test and inspect the product in accordance with ASTH, except for the chemical analysis and mechanical properties of the steel.

Note (2):	Specify ferritizing heat treatment, chemical requirement and mechanical properties, except for tensile and yield strengths.

Note (3): Specify mechanical properties, test and inspection in accordance with ASTM

Note (4):	Recognize lower minimum tensile or yield strengths of the underlined substitute materials in design consideration, or specify minimum tensile and yield strengths per ASTM.

STANDARD SPECIFICATION

| ASTM | JIS | BS | DIN |
| --- | --- | --- | --- |
| A-536 |  |  |  |
| Ductile Iron Castings |  |  |  |
| Gr 60-40-18 | G 5502 FCD450 (1) | 2789 Gr 420/12 | --- |
| Gr 65-45-12 | G 5502 FCD500 (1) | 2789 Gr 500/7 | 1693 GGG-50 |
| Gr 80-55-06 | G 5502 FCD600 (1) | 2789 Gr 600/3 (2) | 1693 GGG-60 |
| Gr 100-70-03 | G 5502 FCD700 (1) | 2789 Gr 700/2 (2) | 1693 GGG-70 |
| A-743 |  |  |  |
| Castings, Iron-Chromium, |  |  |  |
| Iron-Chromium Nickel, |  |  |  |
| Nickel Base, Corrosion Resistant, |  |  |  |
| for General Application |  |  |  |
| Gr CA-15 | G 5121 SCS1 (3) | 3100-410C21 (2) | 17445 G-X20Cr14 |
| Gr CA-40 | G 5121 SCS2 (3) | 1504-420C29 | --- |
|  |  | 3100-420C29 |  |
| Gr CF-3 | G 5121 SCS19A (3) | 1504-344C12 | --- |
|  |  | 3100-304C12 |  |
| Gr CF-3M | G 5121 SCS16A (3) | 1504-316C12 | --- |
|  |  | 3100-316C12 |  |
| Gr CF-8 | G 5121 SCS13A (3) | 1504-304C15 | 17445 G-X6CrNi189 |
|  |  | 3100-304C15 |  |
| Gr CF-8C | G 5121 SCS21 (3) | 1504-347C17 | 17445 G-X5CrNiNb189 |
| Gr CF-8M | G 5121 SCS14A (3) | 1504-316C16 | 17445 G-X6CrNiMo1810 |
|  |  | 3100-316C16 |  |
| Gr CF-20 | G 5121 SCS12 (3) | --- | --- |
| Gr CH-20 | G 5121 SCS17 (3) | 3100-309C30 | --- |
| Gr CK-20 | G 5121 SCS18 (3) | --- | --- |
| Gr CN-7M | G 5121 SCS23 (3) | 1504-332C11 | --- |

Note (1): Specify elongation in accordance with ASTM.

Note (2):	Recognize lower minimum tensile or yield strengths of the underlined substitute materials in design consideration, or specify minimum tensile and yield strengths per ASTM.

Note (3):	Test and inspect the product in accordance with ASTM, except for the chemical analysis and mechanical properties of the steel.

STANDARD SPECIFICATION

Table 6 BOLTS AND NUTS

| ASTM | JIS | BS | DIN |
| --- | --- | --- | --- |
| A-193 |  |  |  |
| Alloy-Steel and Stainless Steel |  |  |  |
| Bolting Materials for High |  |  |  |
| Temperature Service |  |  |  |
| Gr B5 (5Cr) | G 4107 SNB5 | --- | --- |
| Gr B6 (12Cr) | G 4303 SUS410 | 1506-410S21-772 | 1654 X10Cr13 |
| Gr B7 (Cr-Mo) | G 4107 SNB7 | 1506-630-860 | 17200 42CrMo4 |
|  |  |  | 17240 24CrMo5 (3) |
| Gr B7M (Cr-0.2Mo) | G 4107 SNB7 (1) | 1506-630-690 | 17200 42CrMo4 |
|  |  |  | 17240 24CrMo5 (3) |
| Gr B8 | G 4303 SUS304 (2) | 1506-304S31 | 17440 X5CrNi1810 |
| CL 1 (304 sol.trt.) |  |  |  |
| CL 4 (304 str.hd.) |  |  |  |
| Gr B8C | G 4303 SUS347 (2) | 1506-347S31 | 17440 X6CrNiNb1810 |
| CL 1 (347 sol.trt.) |  |  |  |
| CL 2 (347 str.hd.) |  |  |  |
| Gr B8M | G 4303 SUS316 (2) | 1506-316S31 | 17440 X5CrNiMo17122 |
| CL 1 (316 sol.trt.) |  |  |  |
| CL 2 (316 str.hd.) |  |  |  |
| Gr B8T | G 4303 SUS321 (2) | 1506-321S31 | 17440 X6CrNiMTi1810 |
| CL 1 (321 sol.trt.) |  |  |  |
| CL 2 (321 str.hd.) |  |  |  |
| Gr B16 (Cr - Mo - V) | G 4107 SNB16 | 1506-670-860 | 17240 40CrMoV47 |
| A-194 |  |  |  |
| Carbon and Alloy Steel Nuts |  |  |  |
| for Bolts for High-Pressure |  |  |  |
| and High-Temperature Service |  |  |  |
| Gr 2H | G 4051 S45C (3) | 1506-162 | 17240 C35 |
|  |  |  | 1654 Cq45 |
| Gr 4 (C-Mo) | -- | --- | 17240 24CrMo5 |
| Gr 6 (12Cr) | G 4303 SUS410 (3) | 1506-410S21-770 | 1654 X10Cr13 |
| Gr 8 (304) | G 4303 SUS304 (2) | 1506-304S31 | 17440 X5CrNi1810 |
| Gr 8MA (316) | G 4303 Sus316 (2) | 1506-316S31 | 17440 X5CrNiMo17122 |
| A-307 |  |  |  |
| Carbon Steel Externally Threaded |  |  |  |
| Standard Fasteners |  |  |  |
| Gr B | G 3101 SS400 (4) | 4190-Gr 4,6 | 17100 St44.2 |
|  |  |  | 17100 St44.3 |
|  | G 4051 S25C (4) |  | 17200 CK25 |
|  |  |  | 1654 Cq22 |

Note (1): Specify heat treatment and mechanical properties per ASTM.

Note (2): Specify ASTH dimensional requirements, tolerances and inspection.

Note (3): Specify mechanical properties, test and inspection in accordance with ASTM.

Note (4):Test and inspect the product in accordance with ASTM, except for the chemical analysis and mechanical properties of the steel.

STANDARD SPECIFICATION

| ASTM | JIS | BS | DIN |
| --- | --- | --- | --- |
| A-320 |  |  |  |
| Alloy Steel Bolting Materials for |  |  |  |
| Low Temperature Service |  |  |  |
| Gr L7 (Cr-Mo) | G 4107 SNB7 (1) | 1506-630-860 | 17200 42CrMo4 |
|  |  |  | 17240 24CrMo5 |
| Gr L43 (Ni-Cr-Mo) | G 4103 SNCM439 | --- | --- |
| Gr B8 (304 str.hd.) | G 4303 SUS304 (2) | 1506-304S31 | 17440 X5CrNi1810 |
| Gr B8C (347 str.hd.) | G 4303 SUS347 (2) | 1506-347S31 | 17440 X6CrNiNb1810 |
|  |  | 970-347S31 |  |
| Gr B8T (321 str.hd.) | G 4303 SUS321 (2) | 1506-321S31 | 17440 X6CrNiTi1810 |
|  |  | 970-321S31 |  |
| Gr B8M (316 str.hd.) | G 4303 SUS316 (2) | 1506-316S31 | 17440 X5CrNiMo17I22 |
|  |  | 970-316S31 |  |
| A-325 |  |  |  |
| High-Strength Bolts for Structure |  |  |  |
| Steel Joints |  |  |  |
|  | G 4051 S33C | 3139 | 1654 Cq35 |
| A-354 |  |  |  |
| Quenched and Tempered Alloy |  |  |  |
| Steel Bolts, Studs, and Other |  |  |  |
| Externally Threaded Fasteners |  |  |  |
| Gr BC | --- | --- | -- |
| Gr BD | --- | --- | -- |
| A-453 |  |  |  |
| Bolting Materials, High-Temperature |  |  |  |
| , 50 to 120 KSI (345 to 827 Mpa) |  |  |  |
| Yield Strength, with Expansion |  |  |  |
| Coefficients Comparable to |  |  |  |
| Austenitic Steels |  |  |  |
| Gr 660 Class A & B | --- | --- | --- |
| (14Cr-24Ni) |  |  |  |
| Gr 651 Class A & B | --- | --- | --- |
| (19Cr-9Ni) |  |  |  |

Note (1): Specify Impact Test requirement per ASTM.

Note (2): Specify ASTM dimensional requirements, tolerances and inspection.

STANDARD SPECIFICATION

Table 7 BARS AND SHAPES

| ASTM | JIS | BS | DIN |
| --- | --- | --- | --- |
| A-276 |  |  |  |
| Stainless and Heat-Resisting Steel |  |  |  |
| Bars and Shapes |  |  |  |
| Type 420 | G4303 J1 | 970-420S37 | 17440 X20Cr13 |
| A-576 |  |  |  |
| Steel Bars, Carbon, Hot-Wrought |  |  |  |
| Special Quality |  |  |  |
| Gr 1020 | G4051 S20C | --- | 17200 CK22 |
| Gr 1025 | G4051 S25C | --- | 17200 CK25 |
| Gr 1030 | G4051 S30C | --- | 17200 CK30 |
| Gr 1035 | G4051 S35C | --- | 17200 CK35 |
| Gr 1040 | G4051 S40C | --- | 17200 CK40 |
| Gr 1045 | G4051 S45C | --- | 17200 CK45 |
| A-615 |  |  |  |
| Deformed and Plain Billet-Steel |  |  |  |
| Bars for Concrete Reinforcement |  |  |  |
| Gr 40 | G3112 SD295 | Gr 250 (1) | -- |
| Gr 60 | G3112 SD390 (1) | Gr 460/425 (1) | 488 BSt420S |
| A-675 |  |  |  |
| Steel Bars, Carbon, Hot-Wrought, |  |  |  |
| Special Quality, Mechanical |  |  |  |
| Properties |  |  |  |
| Gr 45 | G3101 SS330 | Gr 40A (1) | 17100 St33 |
| Gr 50 | G3101SS330 (1) | Gr 40A (1) | 17100 St33 |
| Gr 55 | G3101 SS400 | Gr 40A (1) | 17100 St44-2 |
|  |  |  | 17100 St44-3 |
| Gr 60 | G3101 SS400 (1) | Gr 43A | 17100 St44-2 |
|  |  |  | 17100 St44-3 |
| Gr 65 | G3101 SS490 | Gr 50A (1) | 17100 St52-3 |
| Gr 70 | G3101 SS490 | Gr 55C or 50A (1) | 17100 St52-3 |
| Gr 75 | G3101 SS540 | Gr 55C or 50A (1) | --- |
| Gr 80 | G3101 SS540 (1) | Gr 55C (1) | --- |

Note (1):	Recognize loser minimum tensile or yield strengths of the underlined substitute materials in design consideration, or specify minimum tensile and yield strengths per ASTM.

STANDARD SPECIFICATION

Table 8 PIPING FITTINGS

| ASTM | JIS | BS | DIN |
| --- | --- | --- | --- |
| A-234 |  |  |  |
| Piping Fittings of Wrought Carbon |  |  |  |
| Steel and Alloy Steel for Moderate |  |  |  |
| and Elevated Temperatures |  |  |  |
| WPB | B 2312 PT410 | 1640 WPB | --- |
|  | 6 2313 PT410W |  |  |
| WPC | B 2312 PT480 | --- | --- |
|  | B 2313 PT480W |  |  |
| WP1 (C-1/2Mo) | B 2312 PA12 | 1640 WP1 | --- |
|  | B 2313 PA12W |  |  |
| WP5 (5Cr-1/2Mo) | B 2312 PA25 | 1640 WP5 | --- |
|  | B 2313 PA25W |  |  |
| WP9 (9Cr-1/2Mo) | 8 2312 PA26 | --- | --- |
|  | B 2313 PA-96W |  |  |
| WP11 (1-1/4Cr-1/2Mo) | B 2312 PA23 | 1640 WP11 | --- |
|  | B 2313 PA23W |  |  |
| WP12 (1Cr-1/2Mo) | B 2312 PA22 | --- | --- |
|  | B 2313 PA22W |  |  |
| WP22 (2-1/4Cr-1Mo) | B 2312 PA24 | 1640 WP22 | --- |
|  | 8 2313 PA24W |  |  |
| A-403 |  |  |  |
| Wrought Austenitic Stainless Steel |  |  |  |
| Piping Fittings |  |  |  |
| WP 304 (18Cr-8Ni) | B2312 SUS304 | 1640-WP304 | --- |
|  | B2313 SUS304W |  |  |
| WP 304H(18Cr-8Ni) | B2312 SUS304H | --- | --- |
| WP 304L (18Cr-8Ni) | B2312 SUS304L | 1640-WP304L | --- |
|  | B2313 SUS304LW |  |  |
| WP 316 (16Cr-12Ni-2Mo) | B2312 SUS316 | 1640-WP316 | --- |
|  | B2313 SUS316W |  |  |
| WP 316H (16Cr-12Ni-2Mo) | B2312 SUS316H | --- | --- |
| WP 316L (16Cr-12Ni-2Mo) | B2312 SUS316L | 1640-WP316L | --- |
|  | B2313 SUS316LW |  |  |
| WP 321 (18Cr-10Ni-Ti) | B2312 SUS321 | 1640-WP321 | --- |
|  | B2313 SUS321W |  |  |
| WP 321H (18Cr-10Ni-Ti) | B2312 SUS321H | --- | --- |
| WP 347 (18Cr-10Ni-Cb) | B2312 SUS347 | 1640-WP347 | --- |
|  | B2313 SUS347W |  |  |
| WP 347H (18Cr-10Ni-Cb) | B2312 SUS347H | --- | --- |

STANDARD SPECIFICATION

|  | JIS | BS | DIN |
| --- | --- | --- | --- |
| A-420 |  |  |  |
| Piping Fittings of Wrought Carbon |  |  |  |
| Steel and Alloy Steel for Low |  |  |  |
| Temperature Service |  |  |  |
| WL3 (3-1/2Ni) | B 2312 PL450 | 1640-WPL3 | --- |
|  | B 2313 PL450W |  |  |
| WL6 | B 2312 PL380 | 1640-WPL0 | --- |
|  | B 2313 PL38OW |  |  |
| WL8 (9Ni) | B 2312 PL690 | --- | --- |

STANDARD SPECIFICATION

Table 9 NONFERROUS MATERIALS

| ASTM | JIS | BS | DIN |
| --- | --- | --- | --- |
| PIPE |  |  |  |
| B-42 |  |  |  |
| Seamless Copper Pipe, Standards | H3300 C1020 | 2871-C103 | 1787 OF-Cu |
| Sizes |  |  |  |
| B-43 |  |  |  |
| Seamless Red Brass Pipe, | H3300 C4430 | --- | 17671 CuZn15 |
| Standard Sizes |  |  |  |
| B-165 |  |  |  |
| Nickel-Copper Alloy Seamless |  |  |  |
| Pipe and Tube |  |  |  |
| N04400 | H4552 NCUT | 3074 | --- |
| B-167 |  |  |  |
| Nickel-Chromium-Iron Alloys |  |  |  |
| Seamless Pipe and Tubes |  |  |  |
| N06600 | G4903 NCF600TP |  |  |
| B-337 |  |  |  |
| Seamless and Welded Titanium |  |  |  |
| and Titanium Alloy pipe |  |  |  |
| Gr 1 | H4630 TTP28 | --- | 17850 Ti1 |
| Gr 2 | H4630 TTP35 | --- | 17850 Ti2 |
| Gr 3 | H4630 TTP49 | --- | 17850 Ti3 |
| Gr 7 | --- | --- |  |
| B-407 |  |  |  |
| Nickel-Iron-Chromium. Alloy |  |  |  |
| Seamless Pipe and Tube |  |  |  |
| N08800 | G4903 NCF 800TP | --- | --- |
| N08810 | G4903 HCF 800HTP | --- | --- |
|  | G4903 NCF 825TP | --- | --- |
| B-466 |  |  |  |
| Seamless Copper-Nickel Pipe |  |  |  |
| and Tube |  |  |  |
| C70600 | H3300 C7060 | 2871-CN102 | 17664 CuNi10Fe1Mn |
| C71500 | H3300 C7150 | 2871-CN107 | 17664 CuNi30Mn1Fe |

STANDARD SPECIFICATION

| ASTM | JIS | BS | DIN |
| --- | --- | --- | --- |
| B-467 Welded Copper-Nickel Pipe |  |  |  |
| C70600 | H3320 C7060 | 2871-CN102 | 17664 CuNi10Fe1Mn |
| C71500 | H3320 C7150 | 2871-CN107 | 17664 CuNi30Mn1Fe |
| CASTINGS |  |  |  |
| B-61 |  |  |  |
| Steam or Valve Bronze Castings | H5111 BC7 | 1400-LG4 | --- |
| B-62 |  |  |  |
| Composition Bronze or Ounce | H5111 BC6 | 1400-LG2 | 1705 G-CuSn5ZnPb |
| Metal Castings |  |  |  |